School of Computer Science & Engineering

Laboratory & Cleanroom Process -

Standard Operating Procedure

ALL FORMS SHOULD BE SUBMITTED ONE WEEK BEFORE THE PROCESS IS TO BE CARRIED OUT.

Spin coating and baking are essential steps in microfabrication for applying photoresist films. During spin coating, a liquid photoresist is dispensed onto a clean substrate, which is then rotated at high speeds to spread the resist uniformly across the surface, with the thickness controlled by the spin speed, resist viscosity, and solvent properties. After coating, the substrate undergoes baking to prepare the resist for subsequent processing. A soft bake (prebake) removes excess solvent, improves adhesion, and reduces stress. After UV exposure, a post-exposure bake is performed to enhance chemical reactions and minimize standing waves. Optionally, a hard bake at higher temperatures (120–200°C) stabilizes the resist for greater resistance to further processing. These steps ensure a uniform, well-adhered resist layer critical for patterning and fabrication.

Brief Description of Process:

- Administration Details:

| User | Sohail Khan, Baidong Wu. Fiza Khan, Zengbo Wang, Liyang Yue |  |  |
| --- | --- | --- | --- |
| Email | shk22gnx@bangor.ac.uk Sohail Khan, eeu984@bangor.ac.uk Baidong Wu, fzk24rqz@bangor.ac.uk Fiza Khan, z.wang@bangor.ac.uk Zengbo Wang, l.yue@bangor.ac.uk Liyang Yue |  |  |
| Room Number | 121A Excimer Laser Room |  |  |
| Supervisor | Liyang Yue, Zengbo Wang | Assessed by |  |
| Date | 12/12/24 | Date |  |
| Signature of User |  |  |  |
| Signature of Supervisor |  | Signature of Assessor |  |

Signatures in the boxes above indicate that both the user, supervisor and assessor are satisfied that the user is competent to carry out the process safely and has received and read any associated COSHH forms.

A 3rd party user is defined as someone from outside the School of Computer Science & Engineering.

By signing this form, you agree to comply with all the safety procedures currently in place in the relevant laboratory/s at the School of Computer Science & Engineering.

You also confirm that you have read and understood the relevant MSDS for all the chemicals involved in this process, and that you will adhere to all control measures on this form.

Any incidents involving spills or hazardous occurrences must be recorded in an accident or near-miss form and reported so that action can be taken to change procedures if necessary.

- Hazards:

Chemical hazards, fire risk, skin & eye irritation

(i) Identity of Hazard

Chemical, physical

(ii) Form of Hazard

25 ppm (100 mg/m³) as an 8-hour time-weighted average

(iii) Exposure limits

Users and people in the lab

(iv) Persons potentially at risk

- Level of Risk (this must be a realistic assessment based on the MSDS):

|  | Likelihood (0-5) | Severity (0-5) | L x S (0-25) | = Risk Level |
| --- | --- | --- | --- | --- |
| Inherent Risk No controls | 2 | 1 | 2 | LOW |
| With Control Measures | 1 | 1 | 1 | LOW |

Note: Level of Risk follows the format used by SAFETY in their risk assessments:

LOW 0 - 7, MEDIUM 8 – 16, HIGH 17 – 25.

- Control Measures

Conduct all work in a fume hood or well-ventilated area. Regular monitoring of temperature, baking time, and solvent level is performed. Work on a spill tray or absorbent surface and keep containers closed when not in use. Always wear PPE chemical-resistant gloves, goggles, and lab coats. Store flammable solvents away from heat sources and ensure no open flames or sparks are present in the workspace. Use heat-resistant gloves when handling hot equipment or substrates.

(Please highlight any additional equipment, gloves and other PPE required):

Procedure

1.1 Preparation

Verify Setup: Ensure the workspace is clean and free from contaminants. Verify the availability of materials and functioning of equipment.

Inspect & Clean Substrate: Check the substrate for defects and clean contaminants before starting.

Preheat Hot Plate: Set the hot plate to the desired pre-bake temperature.

Wear PPE: Put on gloves, safety goggles, lab coat, and any other required PPE.

Fume cupboard & ventilation: Ensure all equipment, e.g. spin coater, hotplate, in fume cupboard and enough ventilation

1.2 Spin Coating Process

Load Substrate: Place the substrate on the chuck of the spin coater. Ensure it is centred to avoid uneven coating.

Dispense Photoresist: Using a pipette or dropper, dispense an adequate amount of photoresist onto the centre of the substrate. The amount depends on the substrate size and desired thickness.

Spin Coating: Program the spin coater with the appropriate parameters (e.g., spin speed and duration). Start the spin coater. Ensure the photoresist spreads uniformly across the substrate.

Inspect Coating: After spinning, visually inspect the substrate under appropriate lighting to ensure uniform coverage and absence of defects.

1.3 Baking (Pre-Bake/Post-Bake) Process

Transfer Substrate: Carefully place the coated substrate onto the preheated hot plate.

Bake Time: Bake the substrate at the specified temperature for the recommended duration.

Cool Down: After baking, allow the substrate to cool to room temperature in a clean environment to prevent contamination or distortion of the photoresist layer.

1.4 Cleanup and Waste Disposal

Dispose of Waste: Discard used photoresist and cleaning materials in waste containers.

Clean Equipment: Wipe down the spin coater and surrounding workspace with cleanroom wipes.

Store Materials: Seal and store photoresist and other chemicals in the chemical storage of the fume cupboard.

Standard Operating Procedure:

- Actions in the case of an accident or emergency associated with the procedure:

1. Chemical Spill

Action:

- Evacuate the area if the spill releases significant solvent vapours or is large.

- Alert others in the vicinity and restrict access to the affected area.

- Use appropriate spill containment materials (e.g., absorbent pads or spill kits).

- Wear proper PPE (gloves, goggles, and respirator if necessary).

- Dispose of spilled material and contaminated items according to the Safety Data Sheet (SDS).

Prevention: Work on a spill tray or absorbent surface and keep containers closed when not in use.

2. Skin or Eye Contact

Action:

- Skin Contact: Wash the affected area with soap and water for at least 15 minutes. Remove contaminated clothing.

- Eye Contact: Flush eyes with water using an eye wash station for at least 15 minutes. Seek medical attention immediately.

Prevention: Always wear chemical-resistant gloves, goggles, and lab coats.

3. Inhalation of Vapours

Action:

- Move the affected person to fresh air immediately.

- Seek medical attention if symptoms like dizziness, nausea, or respiratory distress occur.

- Ensure proper ventilation in the workspace.

Prevention: Conduct all work in a fume hood or well-ventilated area.

4. Fire or Explosion

Action:

- Use a fire extinguisher suitable for chemical fires (Class B or C).

- If the fire is uncontrollable, evacuate the area and activate the fire alarm.

- Shut down heating devices (e.g., hot plates or ovens) if safe to do so.

Prevention: Store flammable solvents away from heat sources and ensure no open flames or sparks are present in the workspace.

5. Thermal Burns (During Baking) Action: - Cool the affected area immediately under running cold water for at least 10–15 minutes. - Do not apply ointments or creams; cover the burn with a sterile dressing. - Seek medical attention for severe burns. Prevention: Use heat-resistant gloves when handling hot equipment or substrates. 6. Chemical Exposure to Clothing Action: - Remove contaminated clothing immediately and isolate it in a chemical waste bag. - Wash exposed skin thoroughly with soap and water. Prevention: Wear a lab coat or apron to protect clothing.